OCTG Heat Treatment Line — Engineering Master v1.1

Canonical Source • PRJ-HTL-01 • Effective 24 Aug 2026

| Field | Value |
| --- | --- |
| Source ID | PRJ-HTL-01-ENG |
| Version | 1.1 |
| Status | CANONICAL_WITH_REVALIDATION_HOLD |
| Authority scope | Stable process/dimensional basis; throughput remains a controlled working value pending engineering revalidation |
| Supersedes | OCTG_Heat_Treatment_Master_v1.0_2026-08-23 |
| Source basis | NEXUS historical engineering requirements + cross-chat reconciliation |

# Stable Engineering Basis

Application: API 5CT steel pipe/OCTG.

Approximate OD: 63.5–177.8 mm.

Wall thickness: 2–20 mm.

Length: 6–12 m.

Process: Quench + Normalize + Temper.

Quench/Normalize furnace: hydraulic walking beam, natural gas, max 960°C; pipe 850–950°C; soak >5 min; uniformity ±10°C; inside/outside ΔT target ±5°C.

Tempering furnace: hydraulic walking beam; max 800°C; pipe 500–750°C; uniformity ±10°C.

Quench: water quench/internal cooling with pumps, heat exchanger and water treatment; line includes roller tables, walking beams, PLC and support/lab systems.

# Throughput Authority — Revalidation Hold

Current NEXUS working value is approximately 40 pipes/hour and must remain isolated from Hydrotester throughput (60 pipes/hour).

However, an older engineer-side message recorded 40–60 pipes/minute. This is materially inconsistent with the later 40 pipes/hour correction.

Operational rule: use ~40 pipes/hour only as CURRENT_WORKING_STATE for analysis and line balancing; before any new RFQ, final technical commitment or contract, revalidate throughput directly with buyer engineering and issue the next canonical revision.

# Other Open Items

Current project activation / management go-ahead.

Any engineering amendments after 21 Aug 2026.

Final utilities, layout, interface, quality/FAT and commissioning requirements.